| Construction |
| --- |
| Item | Material | Diameter(mm) |
| Center Conductor | Bare copper | 1.12 |
| Dielectric | Foam PE | 2.95 |
| 1st Shielding | Bonded Al. Tape | 0.051 (thickness) |
| 2nd Shielding | braiding | 16/7/0.12TC (90%) |
| Jacket | Standard PE | 4.95 |
| Performance |
| Impedance - Ohms | 50±2 |  |
| VSWR | 1.2dB(800-1000MHz, 1700-2200MHz) |  |
| Attenuation(dB/100M) | (8-15% increment is allowed) 30MHz 5.8dB/100m 900MHz 32.6dB/100m 50MHz 7.5 1500MHz 42.4 150MHz 13.1 1800MHz 46.6 220MHz 15.9 2000MHz 49.3 450MHz 22.8 |  |