| Construction |
| --- |
| Item | Material | Diameter(mm) |
| Center Conductor | Copper clad Aluminum | 1.78 |
| Dielectric | Foam PE | 4.83 |
| 1st Shielding | Bonded Al. Tape | 0.051 (thickness) |
| 2nd Shielding | braiding | 90% * 0.15TC |
| Jacket | Standard PE | 7.62 |
| Performance |
| Impedance - Ohms | 50±2 |  |
| VSWR | 1.2dB(800-1000MHz, 1700-2200MHz) |  |
| Attenuation(dB/100M) | (8-15% increment is allowed) 30MHz 3.5dB/100m 900MHz 19.9dB/100m 50MHz 4.5 1500MHz 26 150MHz 7.9 1800MHz 28.7 220MHz 9.6 2000MHz 30.3 450MHz 13.8 |  |